| Item | Standard | Advanced |
| --- | --- | --- |
| Minimum Line/Spacing, Internal | 3/3 | 3/3 |
| Minimum Line/Spacing, External | 4/4 | 3/3 |
| Minimum Drilled Hole Size | 8 | 6 |
| Aspect Ratio (Thickness to Drill) | 10:1 | 15:1 |
| Annular Ring (Diameter over Drill) | 10 | 8 |
| Anti-pad (Diameter over Drill) | 20 | 16 |
| Plated Hole Tolerance | ±3 | ±2 |
| Minimum Dielectric Thickness | 3 | 2 |
| Maximum PCB Thickness (inches) | 0.200 | 0.250 |
| Thickness Tolerance (% of Thickness) | ±10 | ±7 |
| Maximum PCB Dimensions (inches) | 16.0 X 22.0 | 30.0 X 44.0 |
| Fabricated Dimensions - NC Routing | ±5 mils | ±3 |
| Layer-to-Layer Registration Tolerance | ±5 | ±3 |
| Solder Mask Clearance, Per Side | 2.0 mils | 1.5 mils |
| Blind/Buried Vias (All Types) | yes | yes |
| Via Fill (Conductive, Non-Conductive) | no | yes |

| Inner LayersStandardAdvanced | Standard | Advanced |
| --- | --- | --- |
| Minimum Core thickness | 3 mils | 2 mils |
| Minimum Line width | 4 mils | 3 mils (H Oz copper) |
| Minimum Spacing (Air gap) | 4 mils | 3 mils (H Oz copper) |
| Minimum pad size | Drill size +10 mils | Drill size +7 mils |
| Minimum Anti Pad (planes) | Drill size +20 mils | Drill size +16 mils |

| Outer Layers Standard Advanced |  | Standard | Advanced |
| --- | --- | --- | --- |
| Max. Finished Thickness | 0.200 |  | 0.250 |
| Thickness Tolerance | ±10% |  | ±5% |
| Max. Aspect Ratio | 10:1 |  | 12:1 |
| Min. Drill Size | 10 mils |  | 8 mils |
| Min. Line width | 4 mils |  | 3 mils |
| Min. Spacing (air gap) | 4 mils |  | 3 mils |
| Min. Solder mask clearance | 4 mils |  | 3 mils |
| Min. solder mask web thickness | 4 mils |  | 3.4 mils |