| Final Finish Comparison Matrix | Interpretation | Immersion Silver (IAg) | ENIG (Electroless (Ni/Imm Au) | Organic solderability coatings (OSP) | Immersion Tin (ISn) | HASL (no-lead) | HASL (Tin/lead) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Lead free compatible, RoHS compliant | Required | yes | yes | yes | yes | yes | no |
| Solder joint integrity (how good and reliable is the solder joint) |  | very good * | good | good | good | good | best |
| Shelf life (with proper storage**) |  | 12 months** | 12 months | 12 months** | 12 months** | 12 months | 12 months+ |
| Assembly heat cycles (# of passes through reflow) | > is better | multiple | multiple | multiple | multiple | multiple | multiple |
| Fab thermal shock (thermal shock during PCB fabrication) | very low is best | very low | low* | very low | very low | high | high |
| Wettable (how easily does the solder flow onto the surface) |  | very good* | good | good | good | acceptable * | best |
| Solder paste printability (co-planarity of the finish for fine pitch devices) |  | excellent | excellent | excellent | excellent | poor | poor |
| Solder pot compatible (low possibility of solder pot contamination) | desirable | yes | monitor Au concentration | yes | yes | yes | no (if using no lead solder pot) |
| Low contact resistance (resistance of the finish) | yes is good | yes | yes | yes | no | no | no |
| Aluminum wire bonding (can this finish be used with Al wire bonding) | yes is good | yes | yes | no | no | no | no |
| Process cost to PCB fabricator |  | med | high | low | med | high | low |